## Slide 1: Chemical process industries lecture 5 Ceramic
Dr. Intisar Hussain Khalaf

## Slide 2
CERAMIC INDUSTRIES
INTRODUCTION
Ceramic is an inorganic,
nonmetallic solid prepared by the action of heat and subsequent cooling. Ceramic materials may have a crystalline or partly crystalline structure, or may be amorphous (e.g. glass).
Because most common ceramics are crystalline, the definition of ceramic is often restricted to inorganic crystalline materials, as opposed to the non-crystalline glasses.
The word "ceramic" comes from the Greek word Keramos means burnt stuff. Earlier the term ceramic was applied to products made from natural earth material that was not exposed to heat. But nowadays the silicate mainly used in the construction industries and prepared by burning the clay products are called as ceramics.

## Slide 3
CLASSIFICATION
A broad sense classification divides the ceramic products in to two classes
1. Heavy clay products e.g. bricks, roofing tiles, drain tiles, hollow tiles, stoneware and refractories
2. Pottery products e.g. chinaware, wall tiles, electric insulation
Ceramic may also be classified as porous and non-porous. The porosity is depends on particle size, moulding pressure and temperature of vitrification.
Further, ceramic may be classified based on the method of production and its uses into following classes.
1. Whiteware
2. Structural clay products
3. Refractory material
4. Special ceramic products
5. Vitreous enamel

## Slide 4
RAW MATERIAL
The raw materials for ceramics are divided into following groups.
a) Plastics material such as clay
b) Fluxes such as feldspar
c) Non-plastics materials such as silica
a) Clay
Clay gives the main body to the ceramics. The advantage of using clay are
it is plastic when mixed with water becomes hard after drying and
finally it becomes irreversibly solid after firing.
Clay is chosen according to the requirements of particular products and is often blended.
Impurities in common clay incorporate specific qualities as follows.
 Iron oxide in common clay gives red colour to the burnt material
 Lime, magnesia, iron oxide and alkali oxides act as flux which lowers the fusion point of clay
 Silica increases its porosity and refractory nature, while decreases shrinkage
 Clay containing very little and good deals of silica known as fire clays

## Slide 5
b) Feldspar
Feldspar is general name given to the group of minerals. Flux materials like feldspar (Na2OAl2O3.6SiO2) which is easily melting material decreases the melting point of sand or quartz present in the ceramic body. So, that after firing glass like material is obtained called as vitrified material, which is highly impervious and stable to the environment. Fluxes are used for adding vitrifications, reducing porosity, to increase the strength of cold articles and for bonding.
Feldspar is used as fluxing constituent in ceramic formulations along with clay. The common fluxing agents which lower the temperature are borax, boric acid, soda ash, sodium nitrate, potassium carbonate, calcined bones, lead oxides, lithium & barium minerals.
Type of feldspar
 Potash feldspar K2O.Al2O3.6SiO2
 Soda feldspar Na2O.Al2O3.6SiO2
 Lime feldspar CaO.Al2O3.6SiO2

## Slide 6
USES
Ceramic is one of the oldest materials used in construction with the time quality and decoration has been added to its property and therefore they are at present used in following
 Construction and decoration as bricks and tiles
 Metallurgy as construction material of furnace
 Chemical products as stoneware and porcelain
 In drainage of water
 In sanitation
The small uses includes pottery work, specialty ceramic like peuzo electric and insulation material in electrical connections
Therefore, we conclude that ceramics deals with manufacture and technical characteristics and raw material for article building.